Annex A

Parts list, drawings and specifications, Solar Keymark Collectors

Parts list

For each of the collectors of a certification series parts list (bill of materials) must be made available to the inspector / test institute. The parts list shall include all parts of the collector, any changes done to the collector initially tested and the date of revision.

Engineering drawings

Each of the collectors of a certification series must be accompanied by a set of engineering drawings fully dimensioned, including sectional views. Drawings shall have a number, date of issue and possible revision date. These drawings have to include at least the following:

| Flat plate collector | Evacuated tube collector |
| --- | --- |
| ( General view | ( General view |
| ( Casing | ( Tube |
| ( Absorber | ( Absorber |
| ( Transparent cover | ( Reflector |
| ( Insulation | ( Heat transfer sheet |
|  | ( Heat pipe |
|  | ( Manifold |

Specifications

The components listed below must be described and specified using data sheets (alternatively the specification can be documented in the corresponding drawing) that contain at least the following information.

Absorber (flat plate absorber and evacuated tube absorber) ( Material ( Thickness ( absorption and emission of the absorber coating

Transparent cover (flat plate absorber and evacuated tube absorber) ( Material ( Type (e.g. toughened glass, etc.) ( Thickness ( Surface properties (e.g. structure, coatings, etc.) ( solar transmission at normal incidence (air mass 1.5)

Insulations (flat plate absorber and evacuated tube absorber) ( Material ( Type (e.g. open porous, closed porous, etc.) ( Thickness ( Density ( thermal conductivity

Casing (flat plate absorber and evacuated tube absorber) ( Material ( Surface treatment

Heat pipe (evacuated tube absorber) ( Material ( used medium ( fluid content ( pressure

reflector (evacuated tube absorber) ( Material ( Surface treatment (polished, coated, etc.) ( reflectivity

Heat conductive paste (evacuated tube absorber) ( Information about the use of heat conductive paste ( technical specifications

Remarks:

- If several sizes of the same collectors are certified, all documents have to be submitted for all the individual collectors.

- In case of special collector designs the delivery of additional documents might be required.

- The documents are kept strictly confidential by the inspector / test institute. If possible we ask you to submit these drawings by email in pdf format and as hard copy by mail.

- The documents must be supplied to the inspector / test institute either in the language of the country that the inspector / test institute is located or in English.